## Slide 1: Nanophotonics for telecom quantum networks based on neutral silicon vacancy centers in diamond
Ding Huang, Alex Abulnaga, Sacha Welinski, Brendon C. Rose, Zi-Huai Zhang, Paul Stevenson, Nathalie P. de Leon
Department of Electrical Engineering, Princeton University
Diamond substrate
SiV0 Layer
GaAs nanobeam
Frequency (THz)
Requirements for quantum networks:
Long lived quantum memory
Efficient spin-photon interface
Identical photons
Telecom wavelength
Prior work on color centers in diamond:
NV- centers have long electron spin coherence, poor optical properties
SiV- centers have better optical properties, poor spin coherence
Neutral silicon vacancy centers
Key idea—Fermi level engineering to stabilize neutral charge state of SiV, access new spin configuration
SiV0 is a long lived quantum memory:
T1 ~ 1 minute
T2 ~ 1 second
SiV0 is an excellent single photon source:
Near-transform-limited linewidth, low saturation power
Ensemble PLE shows all centers have narrow lines over hours
Heterogeneously integrated GaAs-on-diamond photonic platform
“Observation of an environmentally insensitive solid-state spin defect in diamond”
- Rose*, Huang*, et al, Science, 361, 60-63 (2018)
UV PL
946 nm PL
946 nm optical emission allows for use of GaAs, a mature photonic platform
Evanescent coupling to SiV0 in diamond substrate
Fully integrated nanophotonic circuit using GaAs-on-diamond
Photonic crystal cavity design
Electric field intensity at SiV0 layer around 30% of peak value
Collaboration with Jeff Thompson, Loren Pfeiffer
air
diamond
Number of mirror holes
Quality factor
-400
400
0
0
1
y (nm)
200
-200
0
z (nm)
y = 0 nm
On-chip quantum frequency conversion scheme
Experiments with other material platforms:
Srinivasan group, Nat. Photonics, 2016 (SiN); Radic group, PRL, 2010 (SiO2)
FA9550-17-0158
EFRI
ACQUIRE 1640959
DMR-1420541
YFA program: D18AP00047
Q ~ 104
Intensity (a.u.)
972.5
975
Wavelength (nm)
3 dB attenuation distance in single mode fibers | 
Yb+ ions: 370 nm | < 50 m
NV- center: 637 nm | 300 m
SiV- center: 737 nm | 520 m
Rb atom: 780 nm | 750 m
SiV0 center & QDs: ~946 nm | 1.5 km
Telecom C-band: 1550 nm | 15 km
Pump 1
Pump 2
SiV0
emission
1550 nm
FWM-BS
Wavelength (nm)
Group velocity (a.u.)
SiV0
1550 nm
Notes: Inhomogeneous broadening induced mixing (𝑇_2^∗) allows decay from superradiant state to dark subradiant states.